O & M

MANUAL

MAINTENANCE AND REPAIR OF GFRC

CLEANING

Many GFRC panel projects will require only spot cleaning with soap and water in isolated areas while other projects may require a general cleaning.   More stubborn dirt may require a commercial cleaning compound or a diluted solution of muriatic acid.   Other methods may be used, and all methods should be performed on a small, obscure area before proceeding with full scale work.  The GFRC surface should be wetted in advance to prevent deep absorption of strong cleaners.    A 3% to 5% phosphoric acid solution may be more effective on white concrete and also helps to avoid a yellow stain.  When using acids, special care is required in masking and protecting adjacent materials to avoid damage.   A thorough rinsing with water after use of a strong cleaner is required to neutralize the panel surface.

PATCHING AND REPAIR

A certain amount of repair of product is to be expected as a routine procedure.  Production blemishes should have been corrected at the plant.  Since patching and repair of GFRC is a specialized activity, it is recommended that the manufacturer's personnel be used for repair work.

They understand the use of bonding agents and shading or texturing techniques.   It may even be necessary to prepare a composite patching mix reinforced with glass fibers.   Damage that affects the structural capacity should be discussed with the design engineer.   In general, the extent of patching and repairing required should be minor.

PROCEDURE TO CLEAN PANELS

MATERIAL REQUIRED:

5-Gallon Bucket

Toilet Bowl Cleaner (Ball Heavy Hitter or SSS Emulsion Bowl Cleaner)

Acid Brush and Handle

Pressure Washer

Water

PROCEED AS FOLLOWS:

In 5-gallon bucket, mix one part toilet bowl cleaner to five parts clean water.

Wet panel thoroughly with pressure washer.

Use acid brush and scrub panel with toilet bowl cleaner.

Rinse well with pressure washer, keeping the wand approximately 18-24 inches from the surface.  If the wand is held closer than 18-24 inches, the spray will leave marks on the panel.

INSTRUCTIONS FOR PATCHING

MATERIAL REQUIRED:

2 Bags Patch mix

1 Qt. Forton/Water

Honing Stone

##### Sandpaper

PROCEED AS FOLLOWS:

Mix small amount of patch mix with forton/water to into a thick but workable mixture.  Apply to chipped area, leaving an excessive amount piled.  After 24 hours, hone the area with honing stone.  Use sandpaper to achieve desired texture.

With small chips or holes, it is not necessary to apply an excessive amount to the area to attain the proper texture.